## Slide 1
MICROSTRUCTUAL INVESTIGATION OF SS316L FABRICATED USING POWDER BED FUSION PROCESS
By
Project Members
SARAN MAGESH SHANMUGAVEL M SUBASH K
VISHNU C
-211419114264
-211419114277
-211419114298
- 211419114332
Batch No: 31
Under the Supervision
Of
Mr. J. GUNASEKARAN M.E.,(PhD)
Assistant Professor ,
Department of Mechanical Engineering,
Panimalar Engineering College.

## Slide 2: ABSTRACT
Porosity is one of the major defects threatening mechanical properties in parts manufactured with Selected Laser Melting (SLM) method.
Optimizing densification of materials is thus a key target of SLM as well as other similar methods to achieve the desired properties as per applications.
Globally, SLM is changing the way organizations design and manufacture products. It is an emerging manufacturing technique.
This technique is classified as additive layered manufacturing, as the component is built by adding material in layers.
Components/parts manufactured by Selective Laser Melting (SLM) find a lot of applications in many industries like aerospace, biomedical and automobile.
Proposed research work investigates the effect of various process parameters such as direction of build manufactured by the SLM process of Stainless Steel 316L [SS316L].

## Slide 3: ABSTRACT
The literature indicates that process parameters having maximum impact on mechanical properties includes Laser Power (P), Exposure Time (T), Hatch Spacing (HS).
The effect of these process parameters on Ultimate Tensile Strength (UTS) and its microstructure was investigated.

## Slide 4: ADDITIVE MANUFACTURING
Additive manufacturing is the process by which digital 3D design data is used to build up a component in layers by depositing material. It is opposite to subtractive manufacturing.
According to ASTM F42 additive manufacturing is defined as “the process of joining material to make object from 3D model data usually layer by layer as opposed to subtractive manufacturing methodologies”. Additive manufacturing is also known as “3D printing”.
Additive manufacturing allows for mass customization, reduced material waste, lower cost, increase efficiency compared to injection moulding, extrusion.

## Slide 5: TYPES OF ADDITIVE MANUFACTURING
According to “ASTM F42 – Additive Manufacturing”, formulated a set of standards that classify the range of Additive Manufacturing processes into 7 categories.
Vat photopolymerization
Material jetting
Binder jetting
Material extrusion
Powder bed fusion
Sheet lamination
Directed energy deposition

## Slide 6: LITERATURE SUREVEY
H. Sohrabpoor, V. Salarvand, R.Lupoi, Q.Chu, W.Li, B.aldwell, W.Stanley. Halloran, R. Raghavendra, C.H. Choi, D. Brabazon “Microstructural and mechanical evaluation of post-processed SS 316L manufactured by laser-based powder bed fusion” describe that Post-processing is one of the main ways to improve mechanical and microstructural characteristics of stainless steel 316 L fabricated by the laser-based powder bed fusion (LPBF) process. In this study, optimized LPBF parameters were used to manufacture SS316L bars. For the post-processing, two main heat treatment strategies have been used, quenching and tempering, with various heating and dwelling conditions. While micro-CT scanning was used to identify the porosity inside the as-built specimen, the microstructures of both as-built and heat- treated specimens were additionally investigated by optical microscopy and scanning electron microscopy (SEM).

## Slide 7: LITERATURE SUREVEY
Laser powder bed fusion of 316L stainless steel by ALEXANDER LEICHT describe that One of the most common additive manufacturing techniques for fabricating metallic components is laser powder bed fusion, which has demonstrated great potential in fabricating parts with properties exceeding the properties achieved via conventional methods. To fully utilize the process’s potential, a more profound understanding of the microstructure and properties of the laser powder bed fusion processed material is required. This thesis aims to provide new insights into how the microstructure, mechanical properties and productivity are affected by part design and process parameters. The thesis is framed around a detailed investigation of the parts produced in stainless steel 316L.

## Slide 8: LITERATURE SUREVEY
Xianglong wang, J.A. Muniz-Lerma, Oscar Sanchez Mata, “Microstructure and mechanical properties of stainless steel 316L vertical struts manufactured by laser powder bed fusion process”, describe that Stainless steel 316 L (SS316L) vertical struts with various diameters ranging from 0.25 mm to 5 mm were manufactured by laser powder bed fusion (LPBF) process. A systematic investigation was conducted on the microstructure and mechanical properties of the produced struts. The struts possessed hierarchical microstructures consisting of cellular sub-grain structures inside columnar grains. The primary dendrite arm spacing (PDAS) of the cellular sub-grains decreased monotonically with increasing strut diameter until reaching a plateau after 1 mm. In contrast, the columnar grain width did not show a clear relationship with respect to the variation in the strut diameter.

## Slide 9: LITERATURE SUREVEY
Jian Feng sun, Lu Shen, Weiqiang Wang, Zhu Liu, Huaming Chen, Jieli Duan, “Study of Microstructure and Properties of 316L with Selective Laser Melting Based on Multivariate Interaction Influence”, describe that the selective laser melting technique is widely used in aerospace and biomedical industries, and the performance of formed 316L parts is significantly subject to the forming angle. As the selective laser melting 316L parts are constrained by multiple performance indexes, the study involves multivariate interaction influenced on the forming parameters such as the angle with the xz plane, the angle with the xy plane, laser power, scan speed, powder thickness, and hatching space on the indexes like tensile strength, density, and surface roughness with linear regression equations based on multi objective optimization to obtain the best process parameters.

## Slide 10: LITERATURE SUREVEY
Kanwal Chadha, Yuan Tian, John G. Spray and Clodualdo Aranas Jr., “Effect of Annealing Heat Treatment on the Microstructural Evolution and Mechanical Properties of Hot Isostatic Pressed 316L Stainless Steel Fabricated by Laser Powder Bed Fusion”, describe that in this work, the microstructural features and mechanical properties of an additively manufactured 316L stainless steel have been determined. Three types of samples were characterized: (i) as printed (AP), (ii) annealing heat treated (AHT), and (iii) hot isostatic pressed and annealing heat treated (HIP + AHT). Microstructural analysis reveals that the AP sample formed melt pool boundaries with nano-scale cellular structures. These structures disappeared after annealing heat treatment and hot isostatic pressing. The AP and AHT samples have similar grain morphologies; however, the latter has a lower dislocation density and contains precipitates.

## Slide 11: POWDER BED FUSION
Powder bed fusion process is one of the basic technique associated with additive manufacturing.
It follows the basic principle of manufacturing the product layer by layer and their fusion. A heat source focuses its heat over a powder base material and heats the selected cross section area.
Sources like laser beam, electron beam and infrared beam are used as heating tool.
The process of heating allows the powder to take the shape of the intended object. Powder bed fusion process is compatible to every engineering material such as metals, ceramics polymers, composites etc. this technique is widely used in many industrial sectors such as aerospace, energy sector, transportation etc.

## Slide 12: POWDER BED FUSION
Other popular techniques like selective laser melting (SLM), selective laser sintering (SLS), and electron beam melting (EBM) are also reviewed
Both metal and plastic parts can be made using this method. It can be classified into the following four groups by the energy source it uses to melt the material.
Laser Fused
Electron Beam fused
Fused with agent and energy
Thermally fused
TYPES OF POWDER BED FUSION

## Slide 14: WORKING
A layer, typically 0.1mm thick of material is spread over the build platform.
A laser fuses the first layer or first cross section of the model.
A new layer of powder is spread across the previous layer using a roller.
Further layers or cross sections are fused and added.
The process repeats until the entire model
is created.
Loose, unfused powder is remains in position but is removed during post processing

## Slide 15: POWDER BED FUSION MACHINE
SLM 280 machine
SLM 500 machine

## Slide 16: PROCESS PARAMETER
Build rate = 88cm³/h
Build envelope = 280*280*365 mm
Layer thickness = 0.1mm
Minimum feature size = 150 µm
Maximum scan speed = 10m/s
Weight = 1300kg dry
1800kg with powder
Laser power (volume) = 150W
Scanning speed (volume) = 400mm/s
Laser power (border) =100W
Scanning speed (border) = 300mm/s

## Slide 17: MATERIAL PROPERTIES
Density = 7.90g/cm³
Melting range = 1390-1440°C
Modulus of elasticity = 200GPa
Tensile strength = 650 MN/m2
Yield strength = 280 MN/m2
Young’s modulus = 211 GN/m2
Fatigue limit =.28GN/m2
Elongation at fracture =45
Grade |  | C | Mn | Si | P | S | Cr | Mo | Ni | N
316L | Min (%) | - | - | - | - | - | 16.0 | 2.0 | 10.0 | -
 | Max (%) | .03 | 2.0 | .75 | .045 | .03 | 18.0 | 3.0 | 14.0 | .10

## Slide 18: MANUFACTURING PROCESS
The manufacturing process start from designing the model in software. Software, we used for designing the model is Solidworks and AutoCAD.
After designing the model, the file is converted to STL file format. STL file format plate specimen is shown in figure. Slicing of model are made. STL file format is transferred to SLM machine for building the model. Before the building of model, the settings can constitute power, speed, layer thickness, and other several parameters related to material and process constraints are setup.
Schematic representation of plate

## Slide 19
final components of plate specimen
STL format of plate
Actual building of model is made melting layer by layer. Once the part is
manufactured, it is removed from build platform.

## Slide 20: BASE MATERIAL OF SS316L PLATE

## Slide 21: MICROSTRUCTURE OF SS316L BASE PLATE
shows the optical images of equi axed grains morphology observed in the matrix.
shows the micrograph higher magnification to resolve the grain boundaries.
shows the 500X magnification clearly indicates the grain boundaries are observed.

## Slide 22: ADDITIVELY MANUFACTURED SS316L PLATE

## Slide 23: MICROSTRUCTURE OF ADDITIVELY MANUFACTURED SS316L PLATE
shows the micrograph fish scale morphology observed in the matrix. The matrix columnar grains along the grain boundaries with molten pool observed.
shows the micrograph higher magnification to resolve the columnar sub structure.
shows the 500X magnification clearly indicates the grain boundaries are observed fish scale structure. The fish scale structure remains the grain flow at the grain orientations.
Stainless steel 316L is made in horizontal position in SLM 280 machine.

## Slide 24: ADDITIVELY MANUFACTURED SS316L PLATE WITH HEAT TREATMENT

## Slide 25: MICROSTRUCTURE OF ADDITIVELY MANUFACTURED SS316L PLATE
The non-spherical pores were found to be mainly formed at the interlayer boundaries and are mainly located near the bottom of the melt pools. These types of pores are usually formed due to the excessive energy input and unstable melt low behaviour. Some elongated pores can also be observed. It is also noted that the morphology of the solidified melt pools changes with energy density.
a
b
c
SS316L made in powder bed fusion process in vertical position with heat treatment process.

## Slide 26: THANK YOU!!!